10A NCAC 15 .0114	TESTS FOR SPECIAL FORM

Special form radioactive material as defined in Rule .0104 of this Section must satisfactorily pass the following tests:

(1)	a free drop through a distance of 30 feet onto a flat essentially unyielding horizontal surface, striking the surface in such a position as to suffer maximum damage;

(2)	impact of the flat circular end of a one-inch diameter steel rod weighing three pounds, dropped through a distance on a sheet of lead, of hardness number 3.5 to 4.5 on the Vickers scale, and not more than one inch thick supported by a smooth essentially unyielding surface;

(3)	heating in air to a temperature of 1,475 F. and remaining at that temperature for a period of ten minutes;

(4)	immersion for 24 hours in water at room temperature at pH 6 to pH 8, with a maximum conductivity of ten micromhos per centimeter.

History Note:	Authority G.S. 104E-15;

Eff. February 1, 1980;

Amended Eff. November 1, 1989;

Transferred and Recodified from 10 NCAC 3G .2215 Eff. January 4, 1990;

Amended Eff. May 1, 1993;

Transferred and Recodified from 15A NCAC 11 .0114 Eff. February 1, 2015.